## Slide 1: Probing Electrostatic Interfaces Between van der Waals Materials
AJ Tompkins
REU Program
July 5th, 2022

## Slide 2: What are van der Waals Materials?
Two-dimensional material that emits a weak attractive force
Used in modern day technology
https://www.apple.com/shop/buy-iphone/iphone-13-pro/6.7-inch-display-1tb-sierra-blue-unlocked
Liu, Yuan, Nathan O. Weiss, Xidong Duan, Hung-Chieh Cheng, Yu Huang, and Xiangfeng Duan. “Der Waals Heterostructures and Devices.” Nature Reviews MVanaterials 1, no. 9 (July 12, 2016): 1–17. https://doi.org/10.1038/natrevmats.2016.42.

## Slide 3: How to probe interfaces
Atomic Force Microscopy (AFM)
  Creates topographic image of sample using
  oscillating cantilever
Electrostatic Force Microscopy (EFM)
  Reveals surface potentials of sample
“Imaging the Electrostatic Force with an Atomic Force Microscope.” Accessed July 3, 2022. https://www.nanowerk.com/spotlight/spotid=15905.php.
“What Is AFM? Learn about Atomic Force Microscopy! - NanoAndMore.” Accessed July 3, 2022. https://www.nanoandmore.com/what-is-atomic-force-microscopy.

## Slide 4: Synthesizing heterostructures
hBN
hBN
Gold

## Slide 5: Putting Gold onto Silicon Wafer
Blue squares are silicon wafers
Gold is evaporated onto the wafer

## Slide 6: Stamping
Polymer melts and captures hBN flakes
ResearchGate. “Figure 1. PDMS Stacking Process for Fabrication of VdW Heterostructure....” Accessed July 3, 2022. https://www.researchgate.net/figure/PDMS-stacking-process-for-fabrication-of-vdW-heterostructure-The-flake-exfoliated_fig1_334519290.

## Slide 7: Finding thin flakes
Half are hBN; half are Au_hBN
Microscope is used to find flakes of interest

## Slide 8: Top Layer
Orange flakes are thick; blue flakes are thin
After thin flake is found, polymer is used to capture it

## Slide 9: Bottom Layer
Same process, thin flake is found
Top layer is aligned with the bottom layer

## Slide 10: Completed Heterostructure
hBN_Au_hBN heterostructure
Now the sample can be analyzed via AFM and EFM

## Slide 11: AFM Machine
Cantilever is located under the metallic head at the top
It takes several hours to collect data of the sample

## Slide 12: Analysis of Data
Normal graphs are parabolic, however this one is reciprocal

## Slide 13: Summary
Van der Waal materials have conductive/inductive properties
AFM/EFM are used to measure these properties
Synthesizing heterostructures takes time and patience
In the future, twisted layer graphene will be analyzed
Questions?

## Slide 14: Acknowledgments
University of Kentucky, Department of physics and astrology
Graham lab, Department of Chemistry
Dr. Doug Stratchen
Dr. Beth Guiton
Kathryn Pitton