## Slide 1: Creating the Pellet: SrCoO2.5
By: Mackenzie Walker
Mentor: Dr. Ambrose Seo

## Slide 2: Motivation Behind SrCoO2.5
Antiferromagnetic insulator
  Information is stored in the electrons and in the spin associated with the magnetic moment
  Major interest in field to try and keep long-range spin information communication and storage
Notes: Thin film can hold a lot of information/storage
https://www.nature.com/articles/s43246-020-0022-5

## Slide 3: Step-By-Step
Balance equation with the reactants
Stoichiometry to figure out how much of each reactant is needed to create the target mass of product
X-Ray Diffraction (XRD) to check powders for possible impurities
Calcinate the powder mixture
Powder in Dry Powder Hydraulic Press to create a pellet
Sinter the pellet

## Slide 4: Background: Strontium Cobaltite (SrCoO2.5)
Made using Strontium Carbonate (SrCO3) and Cobalt (II, III) Oxide (Co3O4) powders
12 SrCO3 + 4 Co3O4 12 SrCoO2.5 + 11 CO2 + 1 C
3:1 Ratio
SrCO3
Co3O4
Notes: Add pictures of the powders

## Slide 5: X-Ray Diffractor (XRD)
Co3O4
Determine The Three Dimensional Structure Of Matter. Rigaku. https://www.rigaku.com/techniques/x-ray-diffraction-xrd
Notes: The XRD is a non-destructive technique that can find the crystallographic structure of a material and can find the purity of the samples
It works by emissions of x-rays onto the sample.
  The diffracted x-rays then get collected and then the sample’s structure can be analyzed

## Slide 6
Comparing XRD Data
Co3O4
From XRD
Theoretical using VESTA

## Slide 7
The Y-Axis are arbitrary units
As the X-Values increases, the shift increases
Notes: X values shift difference from about 0.7 degrees to about 2.3 degrees. This does not sound like a lot, but for an xrd graph, it is a lot.
There is also another peak in the graph that should not be there it is the second peak starting from the left. This mean that peak is an impurity

## Slide 8: Mixing the SrCO3 and Co3O4
Target amount of SrCoO2.5 is 2 grams
1.5827g SrCO3 and 0.8605g of Co3O4 needed
1.583g SrCO3 and 0.863g of Co3O4 used
Finely grounded using a mortar and pestle

## Slide 9: Calcination of the SrCO3 + Co3O4
Mixture placed in crucible
Calcinated in furnace at 900ºC for 6 hours
Notes: Calcination is the heating of solids to a high temperature for the purpose of removing volatile substances and oxidizing a portion of mass. It is essentially a method of purification

## Slide 10: SrCO3 + Co3O4 Before Calcination
SrCO3 + Co3O4 After Calcination
Notes: This is it before and after calcination. As seen here, there was not much of a color change

## Slide 11: Creating the Pellet
Powder put into Dry Pellet Pressing Die
Hydraulic Press puts about 36,000 lbs. of pressure for 60 mins. on the powder

## Slide 12: Oops

## Slide 13: Creating the Pellet Again
Powder in Dry Pellet Pressing Die
Hydraulic Press puts about 20,000lbs. of pressure for 60mins.

## Slide 14: Back to the Furnace: Sintering
1100ºC for 24 Hours
Notes: Sintering is a process of forming a solid mass of material and it increases the density. It allows the pellet to keep its properties as it gets tightly fused together

## Slide 15: Summary
Balance equation with the reactants
Stoichiometry to figure out how much of each reactant is needed to create the target mass of product
X-Ray Diffraction (XRD) to check powders for possible impurities
Calcinate the powder mixture
Powder in Dry Powder Hydraulic Press to create a pellet
Sinter the pellet
Questions?